## Slide 1: Liquid Metal Surfaces P. S. Pershan SEAS & Dept of Physics, Harvard Univ., Cambridge, MA, USA
Colleagues
Balagurusamy, V. S. K. Berman, E. Deutsch, M. DiMasi, E. Fukuto, M. Gebhardt , J. Gog, T. Graber, T. Grigoriev, A. | Huber, P. Kawamoto, E. H. Kuzmenko, I. Lin, B. H. Magnussen, O. M. Mechler, S. Meron, M. Ocko, B. M. Pontoni, D. | Regan, M. J. Sellner, S. Shpyrko, O. G. Steimer, C. Stoltz, S. Streitel, R. Tostmann, H. Yahel, E
Harvard, Non-Harvard, Beam Line(Current)

## Slide 2: Liquid Surfaces
Debye-Waller

## Slide 3: Free Surface of Liquid Metal: Hard Wall
Metallic Liquids (D’Evelyn & Rice ‘83)

Layers
Atoms
Ions in
Fermi Sea
Hg
In
Ga
Hg. Magnussen et al. (1995).
Ga Regan et al.(1995).

## Slide 4: Elements Studied
Type I
Type II

## Slide 5: Eutectic Alloys
J. W. Gibbs ~1920 Surface Adsorption: A/B Alloy If Surface Tension: A > B Surface is Rich in “B”.
AxB1-x | g(A)/g(B) | DH* (mixing) | Concentration of Surface Layers |  | 
 |  |  | 1st | 2nd | 34d
GaxBi1-x | 718/378=1.90 | +4 | Liquid-Liquid Phase Sep. |  | 
Ga83.5In16.5 | 718/556=1.29 | +5 | 97%In |  | 
In78Bi22 | 556/378=1.47 | -1 | 35%Bi |  | 
Sn57Bi43 | 560/378=1.48 | +1 | 96%Bi | 25%Bi | 53%Bi
Au71Sn29 | 1100/560=1.96 | -10 | 96%Sn | <1%Sn | 24%Sn
Au72Ge28 | 1100/621=1.77 | -21 | No Gibbs Absorption |  | 
Au82Si18 | 1100/865=1.27 | -30 | 4-layers, 2DXtal (AuSi2) |  | 
Pd81Ge19 | 1500/621=2.4 | -44 | ~40 Å wetting layer (No Measureable Gibbs Absorption) |  | 
*(kJ/mol)Takeuchi and Inoue, Mater. Trans. 46 (2005)

## Slide 6: Gibbs Surface Adsorption(BiSn)
Bi=378, Sn=560,
Alloy: Bi and Sn
(Bi)≈ 398 (Sn)≈567 dyne/cm
Energy Dispersion: f(E)
Adsorption
Scat. Ampl.

## Slide 7: Surface Freezing Au82Si18Eutectic
T
R(1.4 Å-1)
Surface Phases: LT HT1 HT2
LT-GID

## Slide 8: Au82Si18 Truncation Rods
LT Truncation Rod
(Bilayer)
GID vs T
HT2
HT1
LT
Liquid Surface
2D Monolayer
2D Bilayer

## Slide 9: Au82Si18 Interpretation
Diffuse Scattering:
All three phase are liquid
Bi-Layer (LT)
Mono-Layer (HT1)
Best Fits
Qmax smaller
 R(Qx) larger!
Qmax
LT: 0.1Å-1
HT1: 0.5Å-1
HT2: ??
l=1.29Å
a=6.7°
Qz=1.13Å
Qx= 0.012Å-1
π/1.44Å ~2.2Å-1

## Slide 10: AuGe Eutectic(Should be Similar to Au-Si)
 | g(Au)/g(Si or Ge) | DH
Au72Ge28 | 1100/621=1.77 | -21
Au82Si18 | 1100/865=1.27 | -30
Au-Si
Au-Ge
f`(E) @AuL3-Edge
11.05 kev
11.915 kev
Bumphigher density in 1st layer.
No Energy effect  Ge in 1st layer ≤40atm%.
Small Gibbs (Different from Au-Sn, etc)!
No Enhanced Layering or 2D order (Different from Au-Si)!
Au-Si
×0.82

## Slide 11: Pd81Ge19(Dec.’08)
 | Au82Si18 | Pd81Ge19
Glass former | yes | better
DH | -30 | -44
Expected same 2D surface order for Pd81Ge19 as Au82Si18!
Not found; however, something new! Metallic Clusters (Giant Unit Cells)
Small angle oscillations!
Ref: Urban &Feuerbacher,
J.Non-Crys.Sol.(04)
Quenched Icosahedral Clusters
Others: NaCd2 30Å
YbCu4.5 44-49Å
Al3Mg2 28Å
14nm
Mg32(Al,Zn)49
Preliminary fit.
~4%
r/r∞

## Slide 12: Summary
Metal/Vapor InterfaceAtomic Layering:
Surface Structure Factor - F(Qz): Measurement affected by thermal roughness. Requires knowledge of surface tension.
Surface tension: measured with diffuse scattering:
Surface tension effect demonstrated for Ga
Alloys: Surface tension vs. Enthalpy of Mixing Gibbs absorption is not simple. No reliable theory.
Au82Si18 anomalously strong layering and 2D order. Why are Au82Si18, Au72Ge28 and Pd81Ge19 all different?
Need for THEORY!
New Result (Preliminary): Surfaces & Icosahedral Metallic Clusters